537296

Design Floor
Description: DISANO by HARO Project Plank 1-Strip 4VM Crystal Oak brushed 537296
Design: Plank 1-Strip
Style: Crystal Oak
Surface: brushed
Bevel: 4VM
Dimensions mm (HxWxL): 2,00 x 248,00 x 1300,00
PU (boards): 11 piece
PU (M2): 3,540 m²
Level of use (private/commercial): 23 / 33
Installation: Glue-down installation
Made in Germany
Guarantee (private): 25
Blue Angel: yes
ECO Label: ID 0820-11848-008
CE label: yes
Ideal for underfloor heating: yes
Thermal resistance: 0,010 m² K/W
Flammability class: BFLS1
Slip resistance: R9
plasticizer-free
waterproof
Item number: 537296