536055

Laminate
Description: HARO Special Edition NKL31 Graphite Oak text. matt 536055
Style: Graphite Oak
Surface: text. matt
Installation system: Lock Connect plus
Insulation underlay: Silent Pro
Dimensions mm (HxWxL): 9,00 x 193,00 x 1282,00
PU (boards): 7 piece
PU (M2): 1,730 m²
Level of use (private/commercial): 23 / 31
Abrasion resistance: AC3
Installation: Floating installation
Made in Germany
Guarantee (private): 15
Blue Angel: yes
CE label: yes
Ideal for underfloor heating: yes
Thermal resistance: 0,058 m² K/W
Flammability class: CFLS1
Slip resistance: R9
Antistatic class Standard: DIN EN 1815
Impact resistance class: ≥ 8 N / ≥ 500 mm
plasticizer-free
Item number: 536055