540266

Laminate
Description: HARO TRITTY 200 Aqua Gran Via 4V Oak Contura Stone Grey authentic 540266
Design: Gran Via
Style: Oak Contura Stone Grey
Surface: authentic
Bevel: 4V
Installation system: Top Connect
Dimensions mm (HxWxL): 8,00 x 243,00 x 2200,00
PU (boards): 5 piece
PU (M2): 2,680 m²
Level of use (private/commercial): 23 / 33
Abrasion resistance: AC6
Installation: Floating or glue-down installation
Made in Germany
Guarantee (private): 25
Blue Angel: yes
CE label: yes
Ideal for underfloor heating: yes
Thermal resistance: 0,065 m² K/W
Flammability class: CFLS1
Slip resistance: R9
Antistatic class Standard: DIN EN 1815
Impact resistance class: ≥ 15 N / ≥ 1000 mm
plasticizer-free
Suitable for installation in wet areas
Item number: 540266