540286

Laminate
Description: HARO TRITTY 200 Aqua Gran Via 4V Oak Emilia Puro authentic soft 540286
Design: Gran Via
Style: Oak Emilia Puro
Surface: authentic soft
Bevel: 4V
Installation system: Top Connect
Insulation underlay: Silent CT
Dimensions mm (HxWxL): 10,00 x 243,00 x 2200,00
PU (boards): 4 piece
PU (M2): 2,140 m²
Level of use (private/commercial): 23 / 33
Abrasion resistance: AC6
Installation: Floating installation
Made in Germany
Guarantee (private): 25
Blue Angel: yes
CE label: yes
Ideal for underfloor heating: yes
Thermal resistance: 0,065 m² K/W
Flammability class: CFLS1
Slip resistance: R9
Antistatic class Standard: DIN EN 1815
Impact resistance class: ≥ 15 N / ≥ 1000 mm
plasticizer-free
Suitable for installation in wet areas
Item number: 540286