541572

Laminate
Description: HARO TRITTY 200 Aqua Plank 1-Strip 4V Oak Eleganza Antique Grey authentic 541572
Design: Plank 1-Strip
Style: Oak Eleganza Antique Grey
Surface: authentic
Bevel: 4V
Installation system: Top Connect
Insulation underlay: Silent CT
Dimensions mm (HxWxL): 10,00 x 193,00 x 1282,00
PU (boards): 7 piece
PU (M2): 1,730 m²
Level of use (private/commercial): 23 / 33
Abrasion resistance: AC6
Installation: Floating installation
Made in Germany
Guarantee (private): 25
Blue Angel: yes
CE label: yes
Ideal for underfloor heating: yes
Thermal resistance: 0,065 m² K/W
Flammability class: CFLS1
Slip resistance: R9
Antistatic class Standard: DIN EN 1815
Impact resistance class: ≥ 15 N / ≥ 1000 mm
plasticizer-free
Suitable for installation in wet areas
Item number: 541572