534609

Parquet
Description: HARO 3500 HDF Plank 1-Strip 2V Oak Velvet Brown Universal brushed naturaLin plus 534609
Design: Plank 1-Strip
Type of wood: Oak Velvet Brown
Grade: Universal
Surface: brushed naturaLin plus
Bevel: 2V
Installation system: Top Connect
Dimensions mm (HxWxL): 12,00 x 180,00 x 2200,00
Top layer: ca. 2,5 mm
PU (boards): 6 piece
PU (M2): 2,380 m²
Technical construction: 3-layer / HDF coreboard
Installation: Floating or glue-down installation
Made in Germany
Guarantee (private): 15
Blue Angel: yes
CE label: yes
Ideal for underfloor heating: yes
Thermal resistance: 0,071 m² K/W
Flammability class: CFLS1
Slip resistance: R10
Chair caster resistance: DIN EN 425
HARO Parquet 70% PEFC-certified
plasticizer-free
Item number: 534609