538828

Parquet
Description: HARO 4000 Strip Allegro Oak Objekt naturaLin plus 538828
Design: Strip Allegro
Type of wood: Oak
Grade: Objekt
Surface:  naturaLin plus
Installation system: Tongue and Groove
Dimensions mm (HxWxL): 10,00 x 70,00 x 490,00
Top layer: ca. 3,5 mm
PU (boards): 72 piece
PU (M2): 2,470 m²
Technical construction: 2-layer / Solid fingerstrips as middle layer
Installation: Glue-down installation
Guarantee (private): 30
Blue Angel: yes
CE label: yes
Ideal for underfloor heating: yes
Thermal resistance: 0,076 m² K/W
Flammability class: CFLS1
Slip resistance: R10
Chair caster resistance: DIN EN 425
HARO Parquet 70% PEFC-certified
plasticizer-free
Item number: 538828