542123

Parquet
Description: HARO 4000 Plank 1-Strip Duna 4V Oak Sand Grey Sauvage brushed naturaLin plus 542123
Design: Plank 1-Strip Duna
Type of wood: Oak Sand Grey
Grade: Sauvage
Surface: brushed naturaLin plus
Bevel: 4V
Installation system: Tongue and Groove
Dimensions mm (HxWxL): 11,00 x 140,00 x 1500,00
Top layer: ca. 3,5 mm
PU (boards): 11 piece
PU (M2): 2,310 m²
Technical construction: 2-layer / Solid fingerstrips as middle layer
Installation: Glue-down installation
Made in Germany
Guarantee (private): 30
Blue Angel: yes
CE label: yes
Ideal for underfloor heating: yes
Thermal resistance: 0,076 m² K/W
Flammability class: CFLS1
Slip resistance: R10
Chair caster resistance: DIN EN 425
HARO Parquet 70% PEFC-certified
plasticizer-free
Item number: 542123