543502

Parquet
Description: HARO 4000 Plank 1-Strip Prestige Oak Light White Sauvage brushed naturaDur 543502
Design: Plank 1-Strip Prestige
Type of wood: Oak Light White
Grade: Sauvage
Surface: brushed naturaDur
Installation system: Tongue and Groove
Dimensions mm (HxWxL): 10,00 x 120,00 x 1000,00
Top layer: ca. 3,5 mm
PU (boards): 26 piece
PU (M2): 3,120 m²
Technical construction: 2-layer / Solid fingerstrips as middle layer
Installation: Glue-down installation
Guarantee (private): 30
Blue Angel: yes
CE label: yes
Ideal for underfloor heating: yes
Thermal resistance: 0,076 m² K/W
Flammability class: CFLS1
Slip resistance: R10
Chair caster resistance: DIN EN 425
HARO Parquet 70% PEFC-certified
plasticizer-free
Item number: 543502