543555

Parquet
Description: HARO 4000 Strip Classico Smoked Oak Trend brushed naturaDur 543555
Design: Strip Classico
Type of wood: Smoked Oak
Grade: Trend
Surface: brushed naturaDur
Installation system: Tongue and Groove
Dimensions mm (HxWxL): 10,00 x 85,00 x 771,00
PU (boards): 36 piece
PU (M2): 2,380 m²
Technical construction: 2-layer / Solid fingerstrips as middle layer
Installation: Glue-down installation
Guarantee (private): 30
Blue Angel: yes
CE label: yes
Flammability class: CFLS1
Slip resistance: R10
Chair caster resistance: DIN EN 425
HARO Parquet 70% PEFC-certified
plasticizer-free
Item number: 543555